UNIVERSITY OF CALIFORNIA

College of Engineering

Department of Electrical Engineering and Computer Sciences

EE 130/230M	Prof. Liu & Dr. Xu

Spring 2013

Homework Assignment #11 Solutions

Problem 1: MOSFET Subthreshold Leakage Current

For an n-MOSFET with Toxe = 2 nm and WT = 35 nm,

- The subthreshold swing is

- If the normalized current at VGS = 0V is 10 pA, then the threshold current level (100 nA) is 4 decades higher.  Therefore the minimum threshold voltage VT,min = 4 decades × 70 mV/decade = 0.28 V

- If the leakage current specification were to be relaxed to be 100 nA, the minimum threshold voltage would be reduced to 0 V.  For a fixed power supply voltage (maximum gate voltage) VDD, lower VT would result in higher transistor on-state current, i.e. higher effective transistor drive current and hence faster circuit operation.

- Small S is desirable for lower VT hence higher transistor on-state current, for a given off-state leakage current specification.

Problem 2: MOSFET Small Signal Model

- The transconductance of a transistor is the change in output (drain) current that results from a small change in input (gate) voltage.  The equation for MOSFET transconductance is derived from the equation for MOSFET on-state current (in the saturation region of operation) to be

Although VGS-VT increases with increasing gate bias voltage, the field-effect mobility decreases with increasing gate bias voltage (due to increasing transverse electric field) and eventually causes gm to decrease with increasing gate bias voltage.  Therefore, there exists a maximum value of transconductance as a function of the gate bias voltage.

- The intrinsic gain of a MOSFET is

From Slide 18 of Lecture 20, we can see that the channel length modulation parameter  is inversely proportional to the channel length L.  That is, the length of the pinch-off region becomes more significant relative to L, so that the channel length modulation effect of increasing drain current with increasing drain voltage becomes more significant (i.e. gd increases), as L is reduced.  Thus, intrinsic gain degrades with decreasing L for deep-submicron MOSFETs.

Problem 3: Velocity Saturation

- First, we need to find the effective electron mobility, eff .  In order to do so, we need to find the  effective transverse electric field in the inversion layer:

From the plot on Slide 4 of Lecture 20,

The electric field strength at which the electron velocity reaches saturation is

The bulk charge parameter,

- For L = 1 m:

This MOSFET is a long-channel device.

- For L = 0.1m:

This MOSFET is a short-channel device.

( VDsat will decrease with decreasing (VGS-VT)/m or decreasing EsatL.

  - When Toxe decreases, VT decreases (because Cox increases so that the voltage dropped across the gate oxide, Qdep/Cox, decreases) and thus (VGS- VT) increases.  Consequently, VDsat increases.

  - When (VGS(VT) gets smaller, VDsat decreases because it becomes easier to pinch off the inversion-layer channel at the drain end.

Problem 4: MOSFET Short-Channel Effect

- For a n-channel MOSFET with channel dopant concentration NA = 4(1017/cm3, effective oxide thickness Toxe = 3 nm, source/drain junction depth rj = 0.05 (m:

From these calculations of (VT it can be seen that the short channel effect (“VT roll-off”) becomes more severe at shorter gate lengths.

- For a higher value of drain voltage, the drain junction depletion width is larger; so the drain effectively supports a larger fraction of the depletion region charge underneath the gate electrode.  Thus, the short channel effect is enhanced and therefore |VT| decreases more rapidly with decreasing L.