## Slide 1: Agenda for today: Laser cavity design
Today we will use Lumerical FDTD to study a nanowire laser cavity
  Review conditions for lasing in general laser cavity
  Design and analysis of ZnO nanowire laser cavity

## Slide 2: Review: basic laser concepts

## Slide 3: Review: basic laser concepts

## Slide 4: ZnO nanowire laser cavity
As an interesting case study, let’s examine a somewhat exotic laser cavity consisting of a ZnO nanowire laser cavity
“Bottom-up” fabricated ZnO nanowires grown on sapphire substrate
Cavity is formed by mirror between top facet and air and bottom facet and sapphire substrate
How much gain do we need to observe lasing in such a cavity?
Huang, Michael H., et al. "Room-temperature ultraviolet nanowire nanolasers." science 292.5523 (2001): 1897-1899.

## Slide 5: Back-of-the envelope calculation of threshold gain for ZnO nanowire
Sapphire (n = 1.8)
ZnO nanowire (n = 2.45)
Mirror #1
Mirror #2
Assume plane wave normal incidence:
Assume plane wave normal incidence:

## Slide 6: Back-of-the envelope calculation of threshold gain for ZnO nanowire
Sapphire (n = 1.8)
ZnO nanowire (n = 2.45)
Mirror #1
Mirror #2
Assume nanowire length is 10 µm,
confinement factor is unity, and negligible
internal loss
(this is pretty high!)

## Slide 7: Lumerical simulation
Let’s use Lumerical FDTD to get a more accurate value for the mirror reflectivity and confinement factor to determine the threshold gain
We could simulate the entire structure and determine the Q-factor to get the threshold gain however it’s faster to simply simulate the mirror reflectivity for each mirror and use the expression on the previous page

## Slide 8: FDTD procedure
(1) Launch waveguide mode
(3) Monitor reflected power with a field monitor
radiated light
reflected light
(2) Guided mode will reflect off the mirror. Some light will radiate away but some will reflect in the backward direction

## Slide 9: Guided mode source
Open the file ZnO_nanowire_laser_mirror.fsp
This file contains the geometry necessary to simulate reflectivity from both mirrors of the ZnO nanowire cavity
  ZnO has hexagonal cross-section with 130nm diameter
We will assume lasing occurs at the ZnO bangap wavelength of 370nm and therefore center our simulation range at that wavelength

## Slide 10: Computational domain
PML
Mode source
Power monitor
nanowire
air
Movie monitor

## Slide 11: Mode source

## Slide 12: Mode source

## Slide 13: Mode source

## Slide 14: Power monitor

## Slide 15: Power monitor

## Slide 16: Plotting mirror reflectivity
Run simulation (if not already)
Right-click reflectionMonitor and select Visualize  T
This will plot the percentage of power transmitted through the field-monitor. That is it will tell us much power was reflected from the nanowire laser cavity mirror (i.e. reflectivity)

## Slide 17: ZnO-Air mirror reflectivity
11% reflectivity

## Slide 18: ZnO-Air mirror reflectivity
We measure a reflectivity of 11%. This is slightly lower than our back-of-the-envelope calculation of 18%.
Why?

## Slide 19: ZnO-Sapphire reflectivity
Next, we need to simulate the reflectivity of the other mirror.
Click on Layout (where the Run button was) to go back to Layout mode
Right-click on sapphire in the objects tree and click on enable.
Re-run simulation and plot the reflectivity.

## Slide 20: ZnO-Sapphire reflectivity
0.7% reflectivity

## Slide 21: Confinement factor
Finally, we need to determine the confinement factor ( where:
We can do determine the confinement factor by using Lumerical MODE.
Open the file ZnO_nanowire_laser_CF.lms
Click Run, and Calculate modes

## Slide 22: Confinement factor calculation

## Slide 23: Confinement factor calculation
confinement factor

## Slide 24: Confinement factor calculation
We are limited to a circular or rectangular geometry when calculating confinement factor. When waveguide has more complicated geometry (such as ZnO nanowire with hexagonal cross-section) we may wish to more rigorously determine confinement factor by writing a Lumerical script.

## Slide 25: Threshold gain calculation
Now, let’s recalculate the threshold gain calculation with our more accurate values for mirror reflectivity and confinement factor.
Assume nanowire length is 10 µm, and negligible
internal loss
Original estimate was 2800